## Slide 1: XPS results
Qian Zhao
02/09/24

## Slide 2: Elemental composition
Alkaline samples had the least organic C coated on the surface.
Control and Acid samples are comparable.
Minimal S and Cl were detected.
Chart: Atom %
| C1s | O1s | S2p | Cl2p | Fe2p
Control | 11.345 | 63.42 | 0.54333 | 0.081667 | 24.6083
Acid | 9.8567 | 63.48 | 1.02 | 0.35833 | 25.2917
Alkaline | 6.1333 | 64.9133 | 0.11 | 0.21 | 28.635
Salt | 8.1067 | 63.4667 | 0.45667 | 1.0683 | 26.9033
Sample_Name | C1s | O1s | S2p | Cl2p | Fe2p
Ads_061 | 10.755 | 63.785 | 0.41 | 0 | 25.05
Ads_062 | 11.055 | 63.05 | 1.135 | 0.04 | 24.72
Ads_064 | 12.225 | 63.425 | 0.085 | 0.205 | 24.055
Ads_066 | 9.605 | 64.04 | 0.965 | 0.615 | 24.785
Ads_067 | 10.905 | 62.44 | 1.005 | 0.4 | 25.255
Ads_069 | 9.06 | 63.96 | 1.09 | 0.06 | 25.835
Ads_072 | 6.81 | 64.93 | 0.02 | 0.045 | 28.195
Ads_073 | 4.845 | 65.15 | 0.205 | 0.36 | 29.44
Ads_074 | 6.745 | 64.66 | 0.105 | 0.225 | 28.27
Ads_076 | 8.12 | 63.455 | 0.44 | 1.1 | 26.885
Ads_077 | 7.755 | 63.4 | 0.63 | 0.91 | 27.31
Ads_078 | 8.445 | 63.545 | 0.3 | 1.195 | 26.515
Sample_Name | C1s | O1s | S2p | Cl2p | Fe2p
Control | 11.3 | 63.4 | 0.5 | 0.1 | 24.6
Acid | 9.9 | 63.5 | 1.0 | 0.4 | 25.3
Alkaline | 6.1 | 64.9 | 0.1 | 0.2 | 28.6
Salt | 8.1 | 63.5 | 0.5 | 1.1 | 26.9
Average
Elemental Composition

## Slide 3: XPS C1s fitted spectra
Ads_061
Ads_062
Ads_064
Ads_066
Ads_067
Ads_069
Ads_072
Ads_073
Ads_074
Ads_076
Ads_077
Ads_078

## Slide 4: C specie composition
Alkaline samples had the most carbonate on the surface, potentially the least amount of oxidized C (sum of C-O, C=O, and COO functional groups).
Sample_Name | C-C | C-O | C=O | COO | CO3
Control | 15.3 | 32.6 | 35.4 | 11.9 | 4.9
Acid | 13.9 | 39.1 | 31.8 | 9.4 | 5.8
Alkaline | 13.3 | 43.7 | 23.3 | 9.4 | 10.3
Salt | 14.9 | 29.1 | 37.5 | 11.7 | 6.9
Average
C specie composition
Sample_Name | C-C | C-O | C=O | COO | CO3
Ads_061 | 15.8 | 29.0 | 38.3 | 12.1 | 4.8
Ads_062 | 14.5 | 24.1 | 44.7 | 11.8 | 4.9
Ads_064 | 15.5 | 44.5 | 23.1 | 11.7 | 5.1
Ads_066 | 8.7 | 38.0 | 34.2 | 12.1 | 7.0
Ads_067 | 13.2 | 25.1 | 46.6 | 9.8 | 5.3
Ads_069 | 19.8 | 54.2 | 14.7 | 6.2 | 5.1
Ads_072 | 13.8 | 27.7 | 41.1 | 8.7 | 8.7
Ads_073 | 16.6 | 49.8 | 12.6 | 10.2 | 10.9
Ads_074 | 9.4 | 53.6 | 16.4 | 9.3 | 11.3
Ads_076 | 15.8 | 29.0 | 37.1 | 11.5 | 6.6
Ads_077 | 15.9 | 33.8 | 33.0 | 11.4 | 5.8
Ads_078 | 12.9 | 24.4 | 42.3 | 12.2 | 8.3
Chart: Atom %
| C-C | C-O | C=O | COO | CO3
Control | 15.2612 | 32.5588 | 35.3763 | 11.8825 | 4.9211
Acid | 13.8808 | 39.1152 | 31.8245 | 9.3744 | 5.8052
Alkaline | 13.2586 | 43.6863 | 23.3443 | 9.4073 | 10.3034
Salt | 14.8686 | 29.0754 | 37.4753 | 11.6876 | 6.8931